# Compare - Apples to Apples

## Texture Retention

The INVISTA type 6,6 nylon polymer along with the exclusive hollow filament shape of Antron® provide superior resistance to crushing, matting and abrasive wear versus a mill extruded, type 6 nylon fiber.

| This is a mill-extruded type 6 nylon fiber with a trilobal shape. The long lobes of the trilobal are more likely to break prematurely under foot traffic. This causes permanent crushing and matting resulting in poor carpet appearance. |  | Actual floor tests show that repeated traffic has caused permanent damage to the trilobal fiber with cracks, tears and overall fiber degradation. |
| --- | --- | --- |
| This is an Antron® nylon fiber shape. The uniform outer surface provides superior resistance to crushing and matting and abrasive wear. |  | Antron® nylon is not damaged during actual floor tests. Increased resistance to crushing and matting means that a carpet will have superior texture retention over the life of the carpet. |